CC.Fast Blue JHB-736

- PRODUCT:

Name			:  CC.Fast Blue JHB-736

Chemical Class		:  Phtalocyanine Blue α

Colour Index Name	:  Pigment Blue 15:2

Colour Index No.		:  74160 - 74250

CAS No.		:  147-14-8 – 12239-87-1

EINECS No.		:  235-476-0

Substance Name		: Copper chlorophthalocyanine

Molecular Formula	: C32H15ClCuN8

- PHYSICAL PROPERTIES:

Density		:   1,70 – 1,75 gr / cm³		Specific Surface		: 63 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 200 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Red shade alpha-copper phtalocyanine pigment stabilized against flocculation with outstanding fastness properties. Stable to aromatic solvents in paints. Can be used in solvent or liquid pvc/plastisol pigment preparations.

Excellent fastness to weathering.

- APPLICATIONS:

Recommended for all types of solvent paints. Recommended also for paste inks and water based and solvent liquid inks (gravure and flexographic).