CC.Meghafast Blue BD909KNP

- PRODUCT:

Name			:  CC.Meghafast Blue BD909KNP

Chemical Class		:  Phtalocyanine Blue ß

Colour Index Name	:  Pigment Blue 15:3

Colour Index No.		:  74160

CAS No.		:  147-14-8

EINECS No.		: 205-685-1

Substance Name		: 29H,31H-phthalocyaninato(2-)-N29,N30,N31,N32 copper

Molecular Formula	: C32H16CuN8

- PHYSICAL PROPERTIES:

Density		:   1,60 – 1,65 gr / cm³		Specific Surface		: 55 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  30-40 ml / 100 g

pH 		:  6 to 8

Heat stability       :  300 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 300 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Strongest, greenish blue shade beta-copper phthalocyanine pigment with outstanding fastness properties. Stable to aromatic solvents in paints. Can be used in water based paints and pigment preparations.

Suitable for high-tech applications and for most plastics due to high dispersibility. Excellent fastness to weathering.

- APPLICATIONS:

Recommended for all types of inks, paints and plastics. Universal.