CC.Fast Orange G

- PRODUCT:

Name			:  CC.Fast Orange G

Chemical Class		:  Disazopyrazolone

Colour Index Name	:  Pigment Orange 13

Colour Index No.		:  21110

CAS No.		:  3520-72-7

EINECS No.		: 222-530-3

Substance Name		: 4,4'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[2,4-dihydro-5-methyl-2-phenyl-3H-pyrazol-3-one]

Molecular Formula	: C32H24Cl2N8O2

- PHYSICAL PROPERTIES:

Density		:   1,4 – 1,45 gr / cm³		Specific Surface		: 38 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  38 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  4				Tint Tone (1:10)		   : 3

- WEATHER FASTNESS  :

6 Months	:  3				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 2 - 3 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 3 - 4		MEK	: 3 - 4

Butanol		: 3 		Butyl Acetate	: 2 - 3		DOP	: 3 - 4

Toluene		: 2 		White Spirit 	: 4 - 5		DBP	: 4

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 4		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Orange G is an opaque disazopyrazolone pigment. It exhibits high colour strength, high gloss and good printing properties in all printing systems. Not recommended for processing temperatures above 200°C.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.