CC.Fast Orange O

- PRODUCT:

Name			:  CC.Fast Orange O

Chemical Class		:  Dianisidine

Colour Index Name	:  Pigment Orange 16

Colour Index No.		:  21160

CAS No.		:  6505-28-8

EINECS No.		: 229-388-1

Substance Name		: 2,2'-[(3,3'-dimethoxy[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[3-oxo-N-phenylbutyramide]

Molecular Formula	: C34H32N6O6

- PHYSICAL PROPERTIES:

Density		:   1,60 – 1,65 gr / cm³		Specific Surface		: 38 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  40 - 45 ml / 100 g

pH 		:  6 to 8

Heat stability       :  170 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 170 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  3				12 Months		   : 2 - 3

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 3 - 4

Butanol		: 5 		Butyl Acetate	: 4		DOP	: 5

Toluene		: 4 		White Spirit 	: 5		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 3 - 4

- TECHNICAL COMMENTS:

Strong, opaque Orange with good flow.

- APPLICATIONS:

Recommended for liquid  inks packaging and UV inks.

Recommended in powder coating, industrial paints.

Recommended in PVC / Plasticized-PVC.