CC.Fast Orange RL

- PRODUCT:

Name			:  CC.Fast Orange RL

Chemical Class		:  Disazopyrazolone

Colour Index Name	:  Pigment Orange 34

Colour Index No.		:  21115

CAS No.		:  15793-73-4

EINECS No.		: 239-898-6

Substance Name		: 4,4'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[2,4-dihydro-5-methyl-2-(p-tolyl)-3H-pyrazol-3-one]

Molecular Formula	: C34H28Cl2N8O2

- PHYSICAL PROPERTIES:

Density		:   1,4 – 1,45 gr / cm³		Specific Surface		: 58 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  38 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6 - 7				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  3				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Orange RL  is a semi transparent disazopyrazolone pigment. It exhibits high colour strength, high transparency and good allround fastness properties. As it has very good flow properties in paints, it can be used even at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Eminently suitable for the production of opaque orange shades for lead-free and low-lead paints mainly for interior use.