CC.Fast Red BBC

- PRODUCT:

Name			:  CC.Fast Red BBC

Chemical Class		:  Mono Azo Naphthol AS

Colour Index Name	:  Pigment Red 112

Colour Index No.		:  12370

CAS No.		:  6535-46-2

EINECS No.		: 229-440-3

Substance Name		: 3-hydroxy-N-(o-tolyl)-4-[(2,4,5-trichlorophenyl)azo]naphthalene-2-carboxamide

Molecular Formula	: C24H16Cl3N3O2

- PHYSICAL PROPERTIES:

Density		:   1,5 – 1,6 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  42 ml / 100 g

pH 		:  6 to 8

Heat stability       :  150 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 150 C° / 5 min.

Acid Resistance	: 4 - 5				Alkali Resistance		: 4 - 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7				Tint Tone (1:10)		   : 6

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 2 - 3

- FASTNESS PROPERTIES:

Migration             : 3 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 4 		Butyl Acetate	: 3		DOP	: 3 - 4

Toluene		: 3 - 4 		White Spirit 	: 4  		DBP	: 3 - 4

Paraffin Wax	: 4 - 5		Butter		: 3		Soap	:5

Water		: 5		Linseed Oil	: 4		Cellosolve: 3

- TECHNICAL COMMENTS:

CC.Fast Red BBC is a semi opaque Naphthol AS pigment. It exhibits high colour strength and good light and weather fastness properties. Pigment with very good fastness to light and weathering even in medium reductions; therefore an ideal alternative to toluidine red pigments when their fastness properties are not adequate. Provided the risk of blooming is observed it can be used, after the appropriate preliminary trials, in full shades for stoving enamels.

- APPLICATIONS:

Recommended for paste inks as well as for solvent and water based packaging gravure and flexographic printing inks.

Recommended for solvent and water based paints.