CC.Fast Bordeaux PRRC

- PRODUCT:

Name			:  CC.Fast Bordeaux PRRC

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 12

Colour Index No.		:  12385

CAS No.		:  6410-32-8

EINECS No.		: 229-102-5

Substance Name		: 3-hydroxy-4-[(2-methyl-4-nitrophenyl)azo]-N-(o-tolyl)naphthalene-2-carboxamide

Molecular Formula	: C25H20N4O4

- PHYSICAL PROPERTIES:

Density		:   1,35 – 1,40 gr / cm³		Specific Surface		: 25 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  42 ml / 100 g

pH 		:  6 to 8

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 4				Alkali Resistance		: 4

- LIGHT FASTNESS  :

Full Tone (1:1)	:  4 - 5				Tint Tone (1:10)		   : 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 4 		Butyl Acetate	: 4		DOP	: 4 - 5

Toluene		: 3 - 4		White Spirit 	: 5 		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 2		Soap	:5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve: 4

- TECHNICAL COMMENTS:

CC.Fast Bordeaux PRRC is a very blue shade Naphthol AS pigment. It exhibits good light fastness and moderate solvent fastness properties.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Recommended in air drying paints especially in full shade.