CC.Fast Carmine PRCK

- PRODUCT:

Name			:  CC.Fast Carmine PRCK

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 146

Colour Index No.		:  12485

CAS No.		:  5280-68-2

EINECS No.		: 226-103-2

Substance Name		: N-(4-chloro-2,5-dimethoxyphenyl)-3-hydroxy-4-[[2-methoxy-5-[(phenylamino)carbonyl]phenyl]azo]naphthalene-2-carboxamide

Molecular Formula	: C33H27ClN4O6

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  52 ml / 100 g

pH 		:  6 to 8

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 3 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5		MEK	: 4

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Carmine PRCK is a blue shade Naphthol AS pigment. It exhibits good all round fastness properties.

- APPLICATIONS:

Recommended for paste inks as well as for solvent based packaging gravure and flexographic printing inks.

Recommended for  solvent paints.

Suitable in Rubber compounds and PVC/ plastified PVC..