CC.Fast Red F5RK

- PRODUCT:

Name			:  CC.Fast  Red F5RK

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 170

Colour Index No.		:  12475

CAS No.		:  2786-76-7

EINECS No.		: 220-509-3

Substance Name		: 4-[[4-(aminocarbonyl)phenyl]azo]-N-(2-ethoxyphenyl)-3-hydroxynaphthalene-2-carboxamide

Molecular Formula	: C26H22N4O4

- PHYSICAL PROPERTIES:

Density		:   1,4 – 1,45 gr / cm³		Specific Surface		: 19 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  62 ml / 100 g

pH 		:  6 to 8

Heat stability       :  190 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  4 				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5		MEK	: 4

Butanol		: 5 		Butyl Acetate	: 4 - 5		DOP	: 4 - 5

Toluene		: 4 - 5 		White Spirit 	: 5  		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve: 4 - 5

- TECHNICAL COMMENTS:

A very strong, blue shade and semi transparent Naphthol AS pigment. It exhibits excellent light and weather fastness properties as well as good overall fastness properties. As it has very good flow properties in paints, it can also be used at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss. Excellent light fastness properties and good heat stability in polyolefins.

- APPLICATIONS:

Recommended for paste inks as well as for solvent and water based packaging gravure and flexographic printing inks.

Eminently suitable for the production of intense opaque red shades, mainly for general lead-free of low-lead industrial paints and automotive refinishing paints.

Recommend for polyolefins, PVC and PP fibers applications.