CC.Fast Red HFT

- PRODUCT:

Name			:  CC.Fast Red HFT

Chemical Class		:  Benzimidazolone

Colour Index Name	:  Pigment Red 175

Colour Index No.		:  12513

CAS No.		:  6985-92-8

EINECS No.		: 230-249-2

Substance Name		: methyl 2-[[3-[[(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)amino]carbonyl]-2-hydroxy-1-naphthyl]azo]benzoate

Molecular Formula	: C26H19N5O5

- PHYSICAL PROPERTIES:

Density		:   1,50 – 1,55 gr / cm³		Specific Surface		: 74 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  74 ml / 100 g

pH 		:  6 to 8

Heat stability       :  270 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 270 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 				Tint Tone (1:10)		   : 7

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Red 175 is a yellowish red pigment with high transparency, very good fastness to light and weathering and perfect fastness to overpainting by stoving. Mainly for industrial paints, especially transparent and metallic paints. Very good heat resistance properties. Very good fastness to weathering.

- APPLICATIONS:

Mainly for industrial paints, especially transparent and metallic paints.

Recommended for film and fiber applications.

Recommended for paste inks and for solvent- and water based packaging gravure and flexographic printing inks.