CC.Fast Red HF2B

- PRODUCT:

Name			:  CC.Fast Red HF2B

Chemical Class		:  Benzimidazolone

Colour Index Name	:  Pigment Red 208

Colour Index No.		:  12514

CAS No.		:  31778-10-6

EINECS No.		: 250-800-0

Substance Name		: butyl 2-[[3-[[(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)amino]carbonyl]-2-hydroxy-1-naphthyl]azo]benzoate

Molecular Formula	: C29H25N5O5

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 66 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 ml / 100 g

pH 		:  6 to 8

Heat stability       :  250 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 250 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 				Tint Tone (1:10)		   : 6 - 7

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Red 208  is a mid shade, transparent benzimidazolone pigment. It exhibits excellent overall fastness properties.

Standard pigment for PVC. Excellent fastness to weathering. Excellent dielectric properties.

- APPLICATIONS:

Recommended for paste inks and for solvent- and water based packaging gravure and flexographic printing inks.

Recommended for PVC and suitable for polyolefins.