CC.Fast Red PKF

- PRODUCT:

Name			:  CC.Fast Red PFK

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 210

Colour Index No.		:  12477

CAS No.		:  61932-63-6

EINECS No.		:

Substance Name		: 4-[[4-(aminocarbonyl)phenyl]azo]-N-(2-ethoxyphenyl)-3-hydroxynaphthalene-2-carboxamide

Molecular Formula	: C26H22N4O4

- PHYSICAL PROPERTIES:

Density		:   1,4 – 1,45 gr / cm³		Specific Surface		: 19 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  62 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  4 				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 4 		MEK	: 3 - 4

Butanol		: 4 		Butyl Acetate	: 4 		DOP	: 4 - 5

Toluene		: 4 - 5 		White Spirit 	: 5  		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve: 4 - 5

- TECHNICAL COMMENTS:

A very strong, yellow shade and high transparency Naphthol AS pigment. It exhibits excellent light and weather fastness properties as well as good overall fastness properties. As it has very good flow properties in paints, it can also be used at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss.

- APPLICATIONS:

Recommended for NC solvent inks as well as for solvent and water based packaging gravure and flexographic printing inks.