CC.Fast Red PGR

- PRODUCT:

Name			:  CC.Fast Red PGR

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 22

Colour Index No.		:  12315

CAS No.		:  6448-95-9

EINECS No.		:  229-245-3

Substance Name		:  3-hydroxy-4-[(2-methyl-5-nitrophenyl)azo]-N-phenylnaphthalene-2-carboxamide

Molecular Formula	: C24H18N4O4

- PHYSICAL PROPERTIES:

Density		:   1,50 – 1,55 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  42 ml / 100 g

pH 		:  6 to 8

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 4				Alkali Resistance		: 2

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5				Tint Tone (1:10)		   : 4

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3 		MEK	: 3

Butanol		: 3 		Butyl Acetate	: 3		DOP	: 2 - 3

Toluene		: 3 		White Spirit 	: 4 - 5 		DBP	: 2 - 3

Paraffin Wax	: 4 		Butter		: 2		Soap	: 2

Water		: 5		Linseed Oil	: 3		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Red PGR  is a yellow shade, semi transparent Naphthol AS pigment. It exhibits good acid but poor alkali fastness properties. Light fastness is medium.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Recommended in air drying paints especially in full shade.