CC.Fast Carmine PYN

- PRODUCT:

Name			:  CC.Fast  Carmine PYN

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 23

Colour Index No.		:  12355

CAS No.		:  6471-49-4

EINECS No.		: 229-313-2

Substance Name		: 3-hydroxy-4-[(2-methoxy-5-nitrophenyl)azo]-N-(3-nitrophenyl)naphthalene-2-carboxamide

Molecular Formula	: C24H17N5O7

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  46 ml / 100 g

pH 		:  6 to 8

Heat stability       :  130 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 130 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 4

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5				Tint Tone (1:10)		   : 4

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 3		Ethyl Acetate	: 2 		MEK	: 4

Butanol		: 2 		Butyl Acetate	: 2		DOP	: 2 - 3

Toluene		: 3 		White Spirit 	: 4 		DBP	: 2 - 3

Paraffin Wax	: 4 		Butter		: 2		Soap	: 4

Water		: 4		Linseed Oil	: 3		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Carmine PYN  is a very blue shade, semi transparent Naphthol AS pigment. It exhibits good acid and alkali fastness properties. Light fastness is medium.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Recommended in air drying paints especially in full shade.