CC.Fast Red P7RK

- PRODUCT:

Name			:  CC.Fast Red P7RK

Chemical Class		:  Naphthol AS

Colour Index Name	:  Pigment Red 266

Colour Index No.		:  12474

CAS No.		:  36 968-27-1

EINECS No.		: 253-292-9

Substance Name		: 4-[[4-(aminocarbonyl)phenyl]azo]-3-hydroxy-N-(2-methoxyphenyl)naphthalene-2-carboxamide

Molecular Formula	: C25H20N4O4

- PHYSICAL PROPERTIES:

Density		:   1,50 – 1,55 gr / cm³		Specific Surface		: 41 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  -  ml / 100 g

pH 		:  6 to 8

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 4 		MEK	: 3 - 4

Butanol		: 4 - 5 		Butyl Acetate	: 4 - 5		DOP	: 4 - 5

Toluene		: 4  		White Spirit 	: 5  		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Red P7RK is a blue shade Naphthol AS pigment of the P-grade range with extremely low specific conductivity (< 0,2 mS/cm), especially recommended for solvent based packaging printing inks. It exhibits high colour strength, high gloss and high transparency with very good rheological and general fastness properties.

- APPLICATIONS:

Recommended for solvent based packaging printing inks.