CC.Fast Toluidine Ecarlate

- PRODUCT:

Name			:  CC.Fast Toluidine Ecarlate

Chemical Class		:  ß-Naphthol

Colour Index Name	:  Pigment Red 3

Colour Index No.		:  12120

CAS No.		:  2425-85-6

EINECS No.		: 219-372-2

Substance Name		: 1-(4-methyl-2-nitrophenylazo)-2-naphthol

Molecular Formula	: C17H13N3O3

- PHYSICAL PROPERTIES:

Density		:   1,4 – 1,5 gr / cm³		Specific Surface		: 12 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  64 ml / 100 g

pH 		:  5.5 to 7

Heat stability       :  120 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7				Tint Tone (1:10)		   : 3

- WEATHER FASTNESS  :

6 Months	:  3 - 4				12 Months		   : 1

- FASTNESS PROPERTIES:

Migration             : 1 - 2 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 2		MEK	: 2

Butanol		: 3 		Butyl Acetate	: 2 		DOP	: 2

Toluene		: 2 		White Spirit 	: 2 - 3		DBP	: 2

Paraffin Wax	: 4 - 5		Butter		: 2		Soap	:5

Water		: 5		Linseed Oil	: 2 - 3		Cellosolve: 2

- TECHNICAL COMMENTS:

Blue shade opaque beta-Naphthol pigment. It is easy to disperse and exhibits good light- and weather fastness properties.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Recommended in air drying paints especially in full shade.