CC.Fast Red B

- PRODUCT:

Name			:  CC.Fast Red B

Chemical Class		:  Azo

Colour Index Name	:  Pigment Red 38

Colour Index No.		:  21120

CAS No.		:  6358-87-8

EINECS No.		: 228-788-3

Substance Name		: diethyl 4,4'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[4,5-dihydro-5-oxo-1-phenyl-1H-pyrazole-3-carboxylate

Molecular Formula	: C36H28Cl2N8O6

- PHYSICAL PROPERTIES:

Density		:   1,80 gr / cm³			Specific Surface		: 23 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  50  ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6 - 7				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 3 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 3 - 4		MEK	: 1

Butanol		: 3 		Butyl Acetate	: 2		DOP	: 5

Toluene		: 2 		White Spirit 	: 3 		DBP	: 5

Paraffin Wax	: 5		Butter		: 2		Soap	: 3

Water		: 5		Linseed Oil	: 5		Cellosolve: 2

- TECHNICAL COMMENTS:

Very strong yellowish red pigment. Excellent dielectric properties. Not recommended for processing temperatures above 200°C.

- APPLICATIONS:

Recommended for  Rubber compounds.