CC.Fast Signal Red RC

- PRODUCT:

Name			:  CC.Fast  Signal Red RC

Chemical Class		:  ß-Naphthol

Colour Index Name	:  Pigment Red 4

Colour Index No.		:  12085

CAS No.		:  2814-77-9

EINECS No.		: 220-562-2

Substance Name		: 1-[(2-chloro-4-nitrophenyl)azo]-2-naphthol

Molecular Formula	: C16H10ClN3O3

- PHYSICAL PROPERTIES:

Density		:   1,5 – 1,6 gr / cm³		Specific Surface		: 12 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  120 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  4				Tint Tone (1:10)		   : 3

- WEATHER FASTNESS  :

6 Months	:  2 - 3				12 Months		   : 1

- FASTNESS PROPERTIES:

Migration             : 2 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3 - 4		MEK	: 2 - 3

Butanol		: 3 		Butyl Acetate	: 2		DOP	: 2 - 3

Toluene		: 2 - 3 		White Spirit 	: 2 - 3		DBP	: 2 - 3

Paraffin Wax	: 3 - 4		Butter		: 2		Soap	:5

Water		: 5		Linseed Oil	: 4		Cellosolve: 2

- TECHNICAL COMMENTS:

CC.Fast Signal Red RC  is a yellow shade, opaque beta-Naphthol pigment. It is easy to disperse and exhibits good light and weather fastness properties.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Light-red pigment for air-drying paints. Not suitable for stoving enamels because of the high risk of blooming. Severe brown discoloration occurs in epoxy resin finishes.