CC.Fast Scarlet BBN

- PRODUCT:

Name			:  CC.Fast Scarlet BBN

Chemical Class		:  BONA, Ba-laked

Colour Index Name	:  Pigment Red 48:1

Colour Index No.		:  15865:1

CAS No.		:  7585-41-3

EINECS No.		: 228-788-3

Substance Name		: diethyl 4,4'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[4,5-dihydro-5-oxo-1-phenyl-1H-pyrazole-3-carboxylate]

Molecular Formula	: C36H28Cl2N8O6

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  54 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 3				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  4				Tint Tone (1:10)		   : 2 - 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 3 		MEK	: 4 - 5

Butanol		: 4 		Butyl Acetate	: 3		DOP	: 3 - 4

Toluene		: 4 		White Spirit 	: 4 - 5 		DBP	: 3 - 4

Paraffin Wax	: 4 		Butter		: 2		Soap	: 2 - 3

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Red 48:1  is a yellow shade, semi transparent Beta Oxy Naphtoic Acid Ba Laked pigment. It exhibits medium acid and alkali fastness properties and can be used as alternative for Pigment Red 53:1 grades if fastness properties need to be higher.

- APPLICATIONS:

Highly recommended for solvent based packaging gravure inks, it is also suitable for paste inks, water based flexographic printing inks as well as for UV curing systems.