CC.Fast Brilliant Red BHXL

- PRODUCT:

Name			:  CC.Fast Brilliant Red BHXL

Chemical Class		:  BONA, Ca-laked

Colour Index Name	:  Pigment Red 48:2

Colour Index No.		:  15865:2

CAS No.		:  7023-61-2

EINECS No.		: 230-303-5

Substance Name		: calcium 4-[(5-chloro-4-methyl-2-sulphonatophenyl)azo]-3-hydroxy-2-naphthoate

Molecular Formula	: C18H13ClN2O6S.Ca

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 62 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 - 50 ml / 100 g

pH 		:  6 to 8

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 2				Alkali Resistance		: 4 - 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5 		MEK	: 4 - 5

Butanol		: 4 - 5 		Butyl Acetate	: 5		DOP	: 4 - 5

Toluene		: 4 - 5		White Spirit 	: 5 		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Brilliant Red BHXL  is a yellowish, transparent calcium laked beta-Naphthol pigment in the Rubine shade area. It exhibits very good all-round fastness properties.

- APPLICATIONS:

Highly recommended for solvent based packaging gravure inks, it is also suitable for paste inks, water based flexographic printing inks as well as for UV curing systems.