CC.Fast Red 2BCP

- PRODUCT:

Name			:  CC.Fast Red 2BCP

Chemical Class		:  BONA, Ca-laked

Colour Index Name	:  Pigment Red 48:2

Colour Index No.		:  15865:2

CAS No.		:  7023-61-2

EINECS No.		: 230-303-5

Substance Name		: calcium 4-[(5-chloro-4-methyl-2-sulphonatophenyl)azo]-3-hydroxy-2-naphthoate

Molecular Formula	: C18H13ClN2O6S.Ca

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 52 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  40 ml / 100 g

pH 		:  6 to 8

Heat stability       :  240 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 240 C° / 5 min.

Acid Resistance	: 4				Alkali Resistance		: 4 - 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6 - 7				Tint Tone (1:10)		   : 5 - 6

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5 		MEK	: 4 - 5

Butanol		: 4 - 5 		Butyl Acetate	: 5		DOP	: 4 - 5

Toluene		: 4 - 5		White Spirit 	: 5 		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Red 2BCP is a bluish red pigment exhibiting high colour strength, good dispersibility and fastness properties. A highly economical pigment suitable for injection moulding, extrusion, film blowing and PP fibre applications.

- APPLICATIONS:

Recommended for injection moulding, extrusion, film blowing and PP fibre applications.