CC.Fast Red BBM

- PRODUCT:

Name			:  CC.Fast Red BBM

Chemical Class		:  Azo 2B, Mn-laked

Colour Index Name	:  Pigment Red 48:4

Colour Index No.		:  15865:4

CAS No.		:  5280-66-0

EINECS No.		: 226-102-7

Substance Name		: manganese, 4-[(5-chloro-4-methyl-2-sulfophenyl)azo]-3-hydroxy-2-naphthalenecarboxylic acid complex

Molecular Formula	: C18H15ClN2O6S

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 41 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  60 ml / 100 g

pH 		:  6 to 8

Heat stability       :  150 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 150 C° / 5 min.

Acid Resistance	: 3				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5 - 6				Tint Tone (1:10)		   : 3 - 4

- WEATHER FASTNESS  :

6 Months	:  3				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 4 - 5		MEK	: 4

Butanol		: 3 - 4		Butyl Acetate	: 3 - 4		DOP	: 4 - 5

Toluene		: 4 - 5		White Spirit 	: 4  		DBP	: 4 - 5

Paraffin Wax	: 5 		Butter		: 3		Soap	: 2 - 3

Water		: 4 - 5		Linseed Oil	: 3 - 4		Cellosolve: 3 - 4

- TECHNICAL COMMENTS:

Red manganese-laked monoazo pigment with strong transparent colour strength.

- APPLICATIONS:

Recommended for solvent- and water based packaging gravure and flexographic printing inks. Not suitable for inks based on polyamide binders as well as for metal decorating inks.