CC.Fast Red PBMC

- PRODUCT:

Name			:  CC.Fast  Red PBMC

Chemical Class		:  Azo 2B, Mn-laked

Colour Index Name	:  Pigment Red 48:4

Colour Index No.		:  15865:4

CAS No.		:  5280-66-0

EINECS No.		: 226-102-7

Substance Name		: manganese, 4-[(5-chloro-4-methyl-2-sulfophenyl)azo]-3-hydroxy-2-naphthalenecarboxylic acid complex

Molecular Formula	: C18H15ClN2O6S

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  54 ml / 100 g

pH 		:  6 to 8

Heat stability       :  150 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 150 C° / 5 min.

Acid Resistance	: 3				Alkali Resistance		: 2

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6 - 7				Tint Tone (1:10)		   : 3 - 4

- WEATHER FASTNESS  :

6 Months	:  3				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 3 - 4		MEK	: 3 - 4

Butanol		: 3 - 4		Butyl Acetate	: 3 - 4		DOP	: 4

Toluene		: 4 		White Spirit 	: 4  		DBP	: 4

Paraffin Wax	: 5 		Butter		: 2		Soap	: 2 - 3

Water		: 4 - 5		Linseed Oil	: 3 - 4		Cellosolve: 3 - 4

- TECHNICAL COMMENTS:

Red pigment with very good fastness to solvents and overpainting. An important combination pigment for the matching of economical, opaque red shades in combination with molybdate orange, iron oxide red pigments or opaque organic orange/red pigments for general industrial coatings. The manganese content of this pigment can have an influence on the drying behavior of oxidative drying, alkyd resin systems.

- APPLICATIONS:

Highly recommended for solvent based industrial paints An important combination pigment for the matching of economical, opaque red shades in combination with molybdate orange, iron oxide red pigments or opaque organic orange/red pigments for general industrial coatings.