CC.Fast Lithol Scarlet

- PRODUCT:

Name			:  CC.Fast Lithol Scarlet

Chemical Class		:  Azo 2B, Ba-laked

Colour Index Name	:  Pigment Red 49:1

Colour Index No.		:  15630:1

CAS No.		:  1103-38-4

EINECS No.		: 214-160-6

Substance Name		: barium bis[2-[(2-hydroxynaphthyl)azo]naphthalenesulphonate]

Molecular Formula	: C20H14N2O4S.½Ba

- PHYSICAL PROPERTIES:

Density		:   1,30 – 1,35 gr / cm³		Specific Surface		: 55 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  56 ml / 100 g

pH 		:  6 to 8

Heat stability       :  130 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 2

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5				Tint Tone (1:10)		   : 2 - 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 3 (p-PVC)

Ethanol		: 4 		Ethyl Acetate	: 3 		MEK	: 2

Butanol		: 3 - 4 		Butyl Acetate	: 3		DOP	: 3

Toluene		: 3 		White Spirit 	: 3 		DBP	: 3

Paraffin Wax	: 4 		Butter		: 3		Soap	: 2

Water		: 4		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Red 49:1  is a blue shade, semi transparent Azo 2B Ba Laked pigment. It exhibits good acid and poor alkali fastness properties.

- APPLICATIONS:

Highly recommended for solvent based packaging gravure inks and offset inks, it  is also suitable for paste inks.