CC.Fast Lithol Carmine

- PRODUCT:

Name			:  CC.Fast Lithol Carmine

Chemical Class		:  Azo 2B, Ca-laked

Colour Index Name	:  Pigment Red 49:2

Colour Index No.		:  15630:2

CAS No.		:  1103-39-5

EINECS No.		: 214-161-1

Substance Name		: calcium bis[2-[(2-hydroxynaphthyl)azo]naphthalenesulphonate]

Molecular Formula	: C20H14N2O4S.½Ca

- PHYSICAL PROPERTIES:

Density		:   1,20 – 1,25 gr / cm³		Specific Surface		: 38 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  54 ml / 100 g

pH 		:  6 to 8

Heat stability       :  120 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 3 - 4

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5				Tint Tone (1:10)		   : 2 - 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 3 (p-PVC)

Ethanol		: 4 		Ethyl Acetate	: 3 		MEK	: 2

Butanol		: 3 - 4 		Butyl Acetate	: 3		DOP	: 3

Toluene		: 3 		White Spirit 	: 3 		DBP	: 3

Paraffin Wax	: 4 		Butter		: 3		Soap	: 2

Water		: 4		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Red 49:2  is a very blueish shade, semi transparent Azo 2B Ba Laked pigment. It exhibits good acid and poor alkali fastness properties. Same properties than Pigment Red 49:1.

- APPLICATIONS:

Highly recommended for solvent based packaging gravure inks and offset inks, it  is also suitable for paste inks.