CC.Fast Carmine FB

- PRODUCT:

Name			:  CC.Fast Carmine FB

Chemical Class		:  Mono Azo

Colour Index Name	:  Pigment Red 5

Colour Index No.		:  12490

CAS No.		:  6410-41-9

EINECS No.		: 229-107-2

Substance Name		: N-(5-chloro-2,4-dimethoxyphenyl)-4-[[5-[(diethylamino)sulphonyl]-2-methoxyphenyl]azo]-3-hydroxynaphthalene-2-carboxamide

Molecular Formula	: C30H31ClN4O7S

- PHYSICAL PROPERTIES:

Density		:   1,55 – 1,6 gr / cm³		Specific Surface		: 52 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 ml / 100 g

pH 		:  6 to 8

Heat stability       :  160 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 4 - 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  6 - 7				Tint Tone (1:10)		   : 6

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3 - 4		MEK	: 3

Butanol		: 4 		Butyl Acetate	: 4		DOP	: 4

Toluene		: 4		White Spirit 	: 4 		DBP	: 4

Paraffin Wax	: 4 - 5		Butter		: 4- 5		Soap	: 4

Water		: 5		Linseed Oil	: 4		Cellosolve:

- TECHNICAL COMMENTS:

Deep blue shade pigment. It exhibits good acid- and alkali fastness properties.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Recommended for air drying paints.