CC.Fast Rubis 6BS

- PRODUCT:

Name			:  CC.Fast Rubis 6BS

Chemical Class		:  Mono Azo , Ca-laked

Colour Index Name	:  Pigment Red 52:1

Colour Index No.		:  15860:1

CAS No.		:  17852-99-2

EINECS No.		: 241-808-5

Substance Name		: calcium 4-[(4-chloro-5-methyl-2-sulphonatophenyl)azo]-3-hydroxy-2-naphthoate

Molecular Formula	: C18H13ClN2O6S.Ca

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 36 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  52 ml / 100 g

pH 		:  6 to 8

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 4				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5 - 6				Tint Tone (1:10)		   : 2 - 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 3 - 4 (p-PVC)

Ethanol		: 4 		Ethyl Acetate	: 3 		MEK	: 2 - 3

Butanol		: 3 		Butyl Acetate	: 3		DOP	: 3

Toluene		: 4 		White Spirit 	: 4 - 5 		DBP	: 3

Paraffin Wax	: 4 		Butter		: 3		Soap	: 4

Water		: 4		Linseed Oil	: 4 		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Red 52:1  is a blue shade, semi opaque  Mono Azo Ca Laked pigment. It exhibits medium acid and alkali fastness properties.

- APPLICATIONS:

Highly recommended for solvent based packaging gravure inks, it is also suitable for paste inks, and solvent air drying paints