CC.Fast Lake Red C-P

- PRODUCT:

Name			:  CC.Fast Lake Red C-P

Chemical Class		:  ß-Naphthol, Ba-laked

Colour Index Name	:  Pigment Red 53:1

Colour Index No.		:  15585:1

CAS No.		:  5160-02-1

EINECS No.		: 225-935-3

Substance Name		: barium bis[2-chloro-5-[(2-hydroxy-1-naphthyl)azo]toluene-4-sulphonate]

Molecular Formula	: C17H13ClN2O4S.½Ba

- PHYSICAL PROPERTIES:

Density		:   1,50 – 1,60 gr / cm³		Specific Surface		: 64 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  52 ml / 100 g

pH 		:  6 to 8

Acid Resistance	: 4				Alkali Resistance		: 2

- LIGHT FASTNESS  :

Full Tone (1:1)	:  3 - 4				Tint Tone (1:10)		   : 2 - 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5 		MEK	: 5

Butanol		: 5		Butyl Acetate	: 3		DOP	: 4 - 5

Toluene		: 4 - 5		White Spirit 	: 4 - 5 		DBP	: 4 - 5

Paraffin Wax	: 5 		Butter		: 2		Soap	: 2 - 3

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve: 4 – 5

Heat Resistance :     (°C) Approx

|  | PS | HDPE | PP | ABS | PC | PETP |
| --- | --- | --- | --- | --- | --- | --- |
| Full Shade: | 300 | 270 | 300 | 260 | >300 | 300 |
| Tint Shade: | 300 | 270 | 300 | 260 | >300 | 300 |

- TECHNICAL COMMENTS:

Economical yellow shade red pigment with high heat stability and good color strength. Not recommended in applications were good light fastness is required

- APPLICATIONS:

Suitable for the coloration of consumer goods, food packaging and toys.