CC.Fast Lithol Rubine BYB

- PRODUCT:

Name			:  CC.Fast Rubine BYB

Chemical Class		:  BONA, Ca-laked

Colour Index Name	:  Pigment Red 57:1

Colour Index No.		:  15850

CAS No.		:  5281-04-9

EINECS No.		: 226-109-5

Substance Name		: calcium 3-hydroxy-4-[(4-methyl-2-sulphonatophenyl)azo]-2-naphthoate

Molecular Formula	: C18H14N2O6S.Ca

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 52 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  40 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 200 C° / 5 min.

Acid Resistance	: 4				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5				Tint Tone (1:10)		   : 3

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5 		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5		White Spirit 	: 5 		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 3

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

Lithol Rubine BYB is a  transparent yellow shade Calcium laked BONS Red pigment. The shade meets the requirements of process colour magenta.

- APPLICATIONS:

Lithol Rubine BYB  is recommended for paste inks.