CC.Fast Lithol Rubine 2R

- PRODUCT:

Name			:  CC.Fast Rubine 2R

Chemical Class		:  BONA, Ca-laked

Colour Index Name	:  Pigment Red 63:1

Colour Index No.		:  15880:1

CAS No.		:  6417-83-0

EINECS No.		: 229-142-3

Substance Name		: calcium 3-hydroxy-4-[(1-sulphonato-2-naphthyl)azo]-2-naphthoate

Molecular Formula	: C21H14N2O6S.Ca

- PHYSICAL PROPERTIES:

Density		:   1,40 – 1,45 gr / cm³		Specific Surface		: 33 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  50 ml / 100 g

pH 		:  6 to 8

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 3				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  5 - 6				Tint Tone (1:10)		   : 4

- WEATHER FASTNESS  :

6 Months	:  -				12 Months		   : -

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 3 		MEK	: 4 - 5

Butanol		: 4 		Butyl Acetate	: 3		DOP	: 3 - 4

Toluene		: 4 		White Spirit 	: 4 - 5 		DBP	: 3 - 4

Paraffin Wax	: 4 		Butter		: 2		Soap	: 2 - 3

Water		: 4		Linseed Oil	: 3		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Red 63:1  is a deep blue shade, semi transparent BON Ca Laked pigment. It exhibits medium acid and alkali fastness properties.

- APPLICATIONS:

Highly recommended for solvent based packaging gravure inks, it is also suitable for paste inks.

Recommended also for solvent air drying paint.