CC.Fast Violet EPVL

- PRODUCT:

Name			:  CC.Fast  Violet EPVL

Chemical Class		:  Dioxazine Violet

Colour Index Name	:  Pigment Violet 23

Colour Index No.		:  51319

CAS No.		:  6358-30-1

EINECS No.		:  228-767-9

Substance Name		: 8,18-dichloro-5,15-diethyl-5,15-dihydrodiindolo[3,2-b:3',2'-m]triphenodioxazine

Molecular Formula	: C34H22Cl2N4O2

- PHYSICAL PROPERTIES:

Density		:   1,45 – 1,50 gr / cm³		Specific Surface		: 81 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  53 ml / 100 g

pH 		:  6,5 to 7,5

Heat stability       :  280 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 280 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5  		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Violet 23 is a very strong and brilliant blue shade carbazole violet pigment with outstanding fastness properties.

With high tintorial strength and out-standing fastness to light and weathering at a very wide range of concentrations.

It exhibits high colour strength, high gloss, high transparency and flocculation stability with very good rheological properties.

- APPLICATIONS:

Particularly suitable for the shading of the green shade phthalocyanine blue pigments. Recommended for paste inks and for Nitrocellulose solvent for packaging gravure printing inks.