CC.Fast Yellow G

- PRODUCT:

Name			:  CC.Fast Yellow G

Chemical Class		:  Azo

Colour Index Name	:  Pigment Yellow 1

Colour Index No.		:  11680

CAS No.		:  2512-29-0

EINECS No.		: 219-730-8

Substance Name		: 2-[(4-methyl-2-nitrophenyl)azo]-3-oxo-N-phenylbutyramide

Molecular Formula	: C17H16N4O4

- PHYSICAL PROPERTIES:

Density		:   1,4 gr / cm³			Specific Surface		: 21 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  61 ml / 100 g

pH 		:  5.5 to 7

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 3		Butyl Acetate	: 2

Toluene		: 3		White Spirit 	: 5		DBP	: 4

Paraffin Wax	: 4		Butter		: 4

- TECHNICAL COMMENTS:

Pigment Yellow 1 is a strong, opaque monoazo pigment. It exhibits medium light- and weather fastness properties, is easy to disperse and has good stability to recrystallization.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Yellow pigment for air-drying paints. Because the fastness to light and weathering is only moderate, it is used mainly for interior paints. Owing to the high risk of blooming, it is not suitable for stoving enamels.