CC.Fast Yellow OF

- PRODUCT:

Name			:  CC.Fast Yellow OF

Chemical Class		:  Diarylide

Colour Index Name	:  Pigment Yellow 12

Colour Index No.		:  21090

CAS No.		:  6358-85-6

EINECS No.		: 228-787-8

Substance Name		: 2,2'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[3-oxo-N-phenylbutyramide]

Molecular Formula	: C32H26Cl2N6O4

- PHYSICAL PROPERTIES:

Density		:   1,45 – 1,50 gr / cm³		Specific Surface		: 31 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  50 ml / 100 g

pH 		:  6.5 to 7

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  3				Tint Tone (1:10)		   : 3

- WEATHER FASTNESS  :

6 Months	:  2				12 Months		   : 1 - 2

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 		Butyl Acetate	:

Toluene		: 3 - 4		White Spirit 	: 4 - 5		DBP	: 4

Paraffin Wax	: 5		Butter		: 4		Soap	: 5

- TECHNICAL COMMENTS:

Pigment Yellow 12 is a very opaque diarylide yellow pigment. It meets the requirements for the European Scale for Process printing. Excellent flow properties.

- APPLICATIONS:

Main application field is cold set offset printing ink (newspaper printing). Further application fields are other offset printing inks as well as water and solvent based packaging gravure and flexographic printing inks.