CC.Fast Yellow GR-OP

- PRODUCT:

Name			:  CC.Fast Yellow GR-OP

Chemical Class		:  Diarylide

Colour Index Name	:  Pigment Yellow 13

Colour Index No.		:  21100

CAS No.		:  5102-83-0

EINECS No.		: 225-822-9

Substance Name		: 2,2'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[N-(2,4-dimethylphenyl)-3-oxobutyramide]

Molecular Formula	: C36H34Cl2N6O4

- PHYSICAL PROPERTIES:

Density		:   1,2 - 1,4 gr / cm³		Specific Surface		: 38 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 - 55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 190 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 5

Butanol		: 4 - 5		Butyl Acetate	: 5		DOP	: 4 - 5

Toluene		: 4 - 5		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve: 5

- TECHNICAL COMMENTS:

Pigment Yellow 13 GR-OP  is an opaque diarylide yellow pigment. It meets the requirements for the European Scale for Process printing. Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks. Suitable for metal decorating inks when stoving temperature does not exceed 200° C.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks. Suitable for metal decorating inks when stoving temperature does not exceed 200° C.