CC.Fast Yellow H4G

- PRODUCT:

Name			:  CC.Fast Yellow H4G

Chemical Class		:  Monoazo Pigment of the benzimidazolone range

Colour Index Name	:  Pigment Yellow 151

Colour Index No.		:  13980

CAS No.		:  31837-42-0

EINECS No.		: 250-830-4

Substance Name		: 2-[[1-[[(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)amino]carbonyl]-2-oxopropyl]azo]benzoic acid

Molecular Formula	: C18H15N5O5

- PHYSICAL PROPERTIES:

Density		:   1,5 - 1,6 gr / cm³		Specific Surface		: 23 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 - 50 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 160 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5		MEK	: 4 - 5

Butanol		: 4 		Butyl Acetate	: 4		DOP	: 4 - 5

Toluene		: 3 		White Spirit 	: 4 - 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	:4 - 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

Greenish yellow pigment with excellent fastness to light and weathering, especially in deep shades. Relatively good opacity for an organic pigment. As it has very good flow properties in paints, it can also be used at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss. It should be borne in mind that the resistance to very strong alkalis is unsatisfactory.

- APPLICATIONS:

Recommended for  Paint, Automotive Paints.