CC.Fast Yellow H3G

- PRODUCT:

Name			:  CC.Fast Yellow H3G

Chemical Class		:  Monoazo Pigment of the benzimidazolone range

Colour Index Name	:  Pigment Yellow 154

Colour Index No.		:  11781

CAS No.		:  68134-22-5

EINECS No.		: 268-734-6

Substance Name		: N-(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)-3-oxo-2-[[2-(trifluoromethyl)phenyl]azo]butyramide

Molecular Formula	: C18H14 F3N5O3

- PHYSICAL PROPERTIES:

Density		:   1,55 - 1,6 gr / cm³		Specific Surface		: 19 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  55 - 60 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability       :  160 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 160 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5		MEK	: 3 - 4

Butanol		: 4 		Butyl Acetate	: 4 - 5		DOP	: 4 - 5

Toluene		: 4 - 5 		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

Excellent light fastness, heat and solvent stability for a monoazo pigment: upgraded properties are attributed to incorporation of cyclic carbonamide group. Somewhat redder in hue than Benzimidazolone Yellow H4G(P. Yellow 151)

Because of its excellent fastness, it is suitable for use in all concentration ranges down to very pale pastel shades and as a shading pigment. As it has very good flow properties, it can also be used at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss.

- APPLICATIONS:

Recommended for  Paint, Automotive Paints.