CC.Fast Yellow 3GP

- PRODUCT:

Name			:  CC.Fast Yellow 3GP

Chemical Class		:  Bisacetoacetarylide

Colour Index Name	:  Pigment Yellow 155

Colour Index No.		:  200310

CAS No.		:  68516-73-4

EINECS No.		: 271-176-6

Substance Name		: tetramethyl 2,2'-[1,4-phenylenebis[imino(1-acetyl-2-oxoethane-1,2-diyl)azo]]bisterephthalate

Molecular Formula	: C34H32N6O12

- PHYSICAL PROPERTIES:

Density		:   1,40 - 1,45 gr / cm³		Specific Surface		: 52 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  65 - 70 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability       :  260 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 250 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 4 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 5		MEK	: 4 - 5

Butanol		: 5 		Butyl Acetate	: 4 - 5		DOP	: 4 - 5

Toluene		: 4 - 5 		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

Strong, green shade disazo pigment. It exhibits excellent overall fastness properties. Pigment with very high colour strength, good hiding power and good rheological properties.

- APPLICATIONS:

Recommended for paste inks and for solvent- and water based packaging gravure and flexographic printing inks.

Recommended for high quality industrial paints in the yellow, orange and green shade area.

Suitable for PP fibers, packaging and toy applications. Ideal replacement for diarylide and lead chromate pigments.