CC.Fast Yellow WGP

- PRODUCT:

Name			:  CC.Fast Yellow WGP

Chemical Class		:  Azo Salt (Ca)

Colour Index Name	:  Pigment Yellow 168

Colour Index No.		:  13960

CAS No.		:  71832-85-4

EINECS No.		: 276-057-2

Substance Name		: calcium bis[4-[[1-[[(2-chlorophenyl)amino]carbonyl]-2-oxopropyl]azo]-3-nitrobenzenesulphonate]

Molecular Formula	: C16H13ClN4O7S.½Ca

- PHYSICAL PROPERTIES:

Density		:   1,6 - 1,7 gr / cm³		Specific Surface		: 25 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  50 - 55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  260 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 240 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 3 - 4		Ethyl Acetate	: 		MEK	: 3

Butanol		: 4 		Butyl Acetate	: 3 - 4		DOP	: 3 - 4

Toluene		: 3 		White Spirit 	: 4 - 5		DBP	: 4

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 4 - 5		Linseed Oil	: 4 - 5		Cellosolve:

6.   HEAT RESISTANCE :     (°C) Approx

|  | HDPE | PS | ABS |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Transparent : | 260 | 240 | 240 |  |  |  |
| Opaque : | 250 | 240 | 240 |  |  |  |

7.   TECHNICAL COMMENTS:

A cost effective pure green shade yellow with very good light fastness. Good heat resistance and weatherability in full shade allows a wide range of application. Non-warping in HDPE injection moulding.

8.   APPLICATIONS:

Recommended for plastic applications PVC and Polyoléfines.