CC.Fast Yellow GG

- PRODUCT:

Name			:  CC.Fast Yellow GG

Chemical Class		:  Diarylide

Colour Index Name	:  Pigment Yellow 17

Colour Index No.		:  21105

CAS No.		:  4531-49-1

EINECS No.		: 224-867-1

Substance Name		: 2,2'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[N-(2-methoxyphenyl)-3-oxobutyramide]

Molecular Formula	: C34H30Cl2N6O6

- PHYSICAL PROPERTIES:

Density		:   1,3 - 1,4 gr / cm³		Specific Surface		: 23 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 - 55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  200 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 190 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 6

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 4 - 5		Ethyl Acetate	: 3 - 4		MEK	: 3

Butanol		: 		Butyl Acetate	: 3 - 4		DOP	: 3 - 4

Toluene		: 3		White Spirit 	: 4 - 5		DBP	: 4

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Yellow 17 is a green shade transparent diarylide yellow pigment. The shade is somewhat greener than the European Scale for Process printing. It exhibits high transparency and gloss as well as good all round fastness properties in all printing ink systems.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

A very strong, pure and cost effective green shade yellow pigment. Excellent dielectric properties. Not recommended for processing temperatures above 200°C.