CC.Fast Yellow FRN

- PRODUCT:

Name			:  CC.Fast Yellow FRN

Chemical Class		:  Disazo

Colour Index Name	:  Pigment Yellow 170

Colour Index No.		:  21104

CAS No.		:  31775-16-3

EINECS No.		: 250-797-6

Substance Name		: 2,2'-[(3,3'-dichloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[N-(4-methoxyphenyl)-3-oxobutyramide]

Molecular Formula	: C34H30Cl2N6O6

- PHYSICAL PROPERTIES:

Density		:   1,65 - 1,70 gr / cm³		Specific Surface		: 38 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  40 ml / 100 g

pH 		:  7 to 8

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 180 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 				Tint Tone (1:10)		   : 7 - 6

- WEATHER FASTNESS  :

6 Months	:  5 - 4				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 4 - 5 		Butyl Acetate	: 3 - 4		DOP	: 4 - 5

Toluene		: 4 		White Spirit 	: 4 - 5		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	:4 - 5

Water		: 5		Linseed Oil	: 3 - 4		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Yellow 170  is a very strong, red shade disazo yellow. High colour strength, opacity and gloss. Yellow pigment with good fastness to light and weathering for air-drying paints. Very good hiding power as an organic pigment. As it has good rheological properties, it can be used even at high pigment concentrations (about 20 % relative to solid binder) without any effect on gloss. Eminently suitable for the production of intense opaque yellow shades for lead-free or low-lead paints.

- APPLICATIONS:

Recommended for air drying paints and industrial paints.

Suitable for the production of intense opaque yellow shades for lead-free or low-lead paints.