CC.Fast Yellow H6G

- PRODUCT:

Name			:  CC.Fast Yellow H6G

Chemical Class		:  Benzimidazolone

Colour Index Name	:  Pigment Yellow 175

Colour Index No.		:  11784

CAS No.		:  35636-63-6

EINECS No.		: 252-650-1

Substance Name		: dimethyl 2-[[1-[[(2,3-dihydro-2-oxo-1H-benzimidazol-5-yl)amino]carbonyl]-2-oxopropyl]azo]terephthalate

Molecular Formula	: C21H19N5O7

- PHYSICAL PROPERTIES:

Density		:   1,50 - 1,55 gr / cm³		Specific Surface		: 28 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  65 - 70 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 160 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  8				Tint Tone (1:10)		   : 7 - 8

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 4		MEK	: 3 - 4

Butanol		: 4 - 5		Butyl Acetate	: 4 - 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5 		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 4 - 5

- TECHNICAL COMMENTS:

Pigment Yellow 175  is a green shade, opaque benzimidazolone pigment with excellent light, weather and solvent fastness properties as well as high heat stability. As it has very good flow properties, it can also be used at high pigment concentrations (25 - 30 % pigment relative to solid binder) without affecting the gloss. Of interest for brilliant green shades in combination with phthalocyanine pigments.

APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

In Paints Of interest for brilliant green shades in combination with phthalocyanine pigments.