CC.Fast Yellow RL

- PRODUCT:

Name			:  CC.Fast Yellow RL

Chemical Class		:  Azo Pigment

Colour Index Name	:  Pigment Yellow 183

Colour Index No.		:  18792

CAS No.		:  65212-77-3

EINECS No.		:  265-634-4

Substance Name		: Calcium 4,5-dichloro-2-[[4,5-dihydro-3-methyl-5-oxo-1-(3-sulphonatophenyl)-1H-pyrazol-4-yl]azo]benzenesulphonate

Molecular Formula	: C16H12Cl2N4O7S2.Ca

- PHYSICAL PROPERTIES:

Density		:   1,80 - 1,85 gr / cm³		Specific Surface		: 18 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  53 ml / 100 g

pH 		:  5 to 6

Heat stability       :  280 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 280 C° / 5 min.

Acid Resistance	: 4 - 5				Alkali Resistance		: 4 - 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 8				Tint Tone (1:10)		   : 7

- WEATHER FASTNESS  :

6 Months	:  4 - 5				12 Months		   : 4 - 5

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4 - 5		MEK	: 3 - 4

Butanol		: 5 		Butyl Acetate	: 4 - 5		DOP	: 5

Toluene		: 5 		White Spirit 	: 5		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 5		Cellosolve: 4 - 5

- TECHNICAL COMMENTS:

Redish yellow pigment with excellent fastness properties. Applications in a wide range of polymers. Replacement for cadmium, lead chromate and diarylide pigments.

- APPLICATIONS:

Recommended for Plastics mainly. Suitable for paints.