CC.Fast Yellow LBF

- PRODUCT:

Name			:  CC.Fast Yellow LBF

Chemical Class		:  Diarylide Mix

Colour Index Name	:  Pigment Yellow 188

Colour Index No.		:  21094

CAS No.		:  23792-68-9

EINECS No.		:  276-057-2

Substance Name		:

Molecular Formula	:

- PHYSICAL PROPERTIES:

Density		:   1,45 - 1,50 gr / cm³		Specific Surface		: 29 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  55 - 60 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 120 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  4 - 5				Tint Tone (1:10)		   : 3 - 4

- WEATHER FASTNESS  :

6 Months	:  2				12 Months		   : 2

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3		MEK	: 5

Butanol		: 5 		Butyl Acetate	: 3		DOP	: 5

Toluene		: 3 		White Spirit 	: 5		DBP	: 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	: 5

Water		: 5		Linseed Oil	: 4 - 5		Cellosolve:

- TECHNICAL COMMENTS:

A transparent, mid shade yellow with very good flow properties and excellent gloss.

- APPLICATIONS:

Recommended for  Offset Inks.