CC.Fast Yellow HGP

- PRODUCT:

Name			:  CC.Fast  Yellow HGP

Chemical Class		:  Mono Azo Pyrazolone, Ca Lake

Colour Index Name	:  Pigment Yellow 191:1

Colour Index No.		:  18795:1

CAS No.		:  154946-66-4

EINECS No.		:  -

Substance Name	   : 4-Chloro-2-[[5-hydroxy-3-methyl-1-(3- sulfophenyl)-1H-pyrazol-4-yl]azo]-5- methylbenzenesulfonic acid, diammonium salt (1:2)

Molecular Formula	: C10H10N2O4 S

- PHYSICAL PROPERTIES:

Density		:   1,75 - 1,80 gr / cm³		Specific Surface		: 20 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :

pH 		:  6 to 8

Heat stability       :  300 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 300 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 				Tint Tone (1:10)		   : 6 - 7

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 5 (p-PVC)

Ethanol		: 		Ethyl Acetate	: 		MEK	:

Butanol		:  		Butyl Acetate	: 		DOP	: 5

Toluene		: 		White Spirit 	: 		DBP	: 5

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

Economical red-shade yellow pigment with excellent heat stability and resistance properties.

- APPLICATIONS:

Recommended for  Plastics. Yellow pigment with excellent fastness properties. Applications in a wide range of polymers. Replacement for cadmium, lead chromate and diarylide pigments.

.