CC.Fast Yellow 10GC

- PRODUCT:

Name			:  CC.Fast Yellow 10GC

Chemical Class		:  Mono Azo

Colour Index Name	:  Pigment Yellow 3

Colour Index No.		:  11710

CAS No.		:  6486-23-3

EINECS No.		: 229-355-1

Substance Name		: 2-[(4-chloro-2-nitrophenyl)azo]-N-(2-chlorophenyl)-3-oxobutyramide

Molecular Formula	: C16H12Cl2N4O4

- PHYSICAL PROPERTIES:

Density		:   1,6 gr / cm³			Specific Surface		: 11 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  59 ml / 100 g

pH 		:  5.5 to 7

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 				Tint Tone (1:10)		   : 7 - 6

- WEATHER FASTNESS  :

6 Months	:  5				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 3 - 4 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3 - 4		MEK	: 3 - 4

Butanol		: 2		Butyl Acetate	: 2

Toluene		: 4		White Spirit 	: 5		DBP	: 3

Paraffin Wax	: 4 - 5		Butter		: 3		Soap	: 5

- TECHNICAL COMMENTS:

Pigment Yellow 3 is a very green shade, opaque mono azo pigment. It exhibits good light- and weather fastness properties.

Pigment with good fastness to light and weathering for air-drying paints. Because of its pure greenish shade it is particularly suitable for green mixtures.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Yellow pigment for air-drying paints. Because the fastness to light and weathering is only moderate, it is used mainly for interior paints. Owing to the high risk of blooming, it is not suitable for stoving enamels.