CC.Fast Yellow 6500C

- PRODUCT:

Name			: CC.Fast Yellow 6500 C

Chemical Class		:  Arylid

Colour Index Name	:  Pigment Yellow 65

Colour Index No.		:  11740

CAS No.		:  6528-34-3

EINECS No.		: 229-419-9

Substance Name		: 2-[(4-methoxy-2-nitrophenyl)azo]-N-(2-methoxyphenyl)-3-oxobutyramide

Molecular Formula	: C18H18N4O6

- PHYSICAL PROPERTIES:

Density		:   1,2 - 1,4 gr / cm³		Specific Surface		: 39 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  45 - 55 ml / 100 g

pH 		:  6.5 to 7.5

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 150 C° / 5 min.

Acid Resistance	: 4				Alkali Resistance		: 3

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 4		Ethyl Acetate	: 4		MEK	: 5

Butanol		: 4 		Butyl Acetate	: 5		DOP	: 4

Toluene		: 3 - 4 		White Spirit 	: 4 		DBP	: 4

Paraffin Wax	: 5		Butter		: 5		Soap	: 3

Water		: 5		Linseed Oil	: 5		Cellosolve: 3

- TECHNICAL COMMENTS:

A very strong and economical classical yellow pigment with excellent dielectric properties. Not recommended for processing temperatures above 200°C.

- APPLICATIONS:

Recommended for  Paint, Industrial and Decorative Paints.