CC.Fast Yellow 4GX

- PRODUCT:

Name			:  CC.Fast Yellow 4GX

Chemical Class		:  Mono Azo

Colour Index Name	:  Pigment Yellow 73

Colour Index No.		:  11738

CAS No.		:  13515-40-7

EINECS No.		: 236-852-7

Substance Name		: 2-[(4-chloro-2-nitrophenyl)azo]-N-(2-methoxyphenyl)-3-oxobutyramide

Molecular Formula	: C17H15ClN4O5

- PHYSICAL PROPERTIES:

Density		:   1,4 - 1,5 gr / cm³		Specific Surface		: 21 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  55 - 65 ml / 100 g

pH 		:  6 to 8

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  4				12 Months		   : 3 - 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 3 - 4		MEK	: 3

Butanol		: 3 - 4 		Butyl Acetate	: 2 - 3		DOP	: 3 - 4

Toluene		: 3 		White Spirit 	: 5		DBP	: 3 - 4

Paraffin Wax	: 4		Butter		: 4		Soap	:5

Water		: 5		Linseed Oil	: 4		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Yellow 73  is a green shade monoazo pigment. The shade is similar to Pigment Yellow 1 but with higher transparency and good light- and weather fastness properties. Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks. Yellow pigment for air-drying paints. Of particular importance is its stability to recrystallization which is excellent compared with other Mono Azo Yellow grades and makes it eminently suitable for the production of tinting colours for emulsion paints and air-drying synthetic resin paints.

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Because of the high risk of blooming it is not suitable for stoving enamels.