CC.Fast Yellow 2GP07

- PRODUCT:

Name			:  CC.Fast Yellow 2GP07

Chemical Class		:  Mono Azo

Colour Index Name	:  Pigment Yellow 74

Colour Index No.		:  11741

CAS No.		:  6358-31-2

EINECS No.		: 228-768-4

Substance Name		: 2-[(2-methoxy-4-nitrophenyl)azo]-N-(2-methoxyphenyl)-3-oxobutyramide

Molecular Formula	: C18H18N4O6

- PHYSICAL PROPERTIES:

Density		:   1,4 - 1,5 gr / cm³		Specific Surface		: 18 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  50 - 55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  5 - 4				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 3 - 4 		Butyl Acetate	: 3		DOP	: 4

Toluene		: 4 		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

Pigment Yellow 74 is a very strong, green shade highly opaque monoazo yellow. Yellow pigment with good fastness to light and weathering for air-drying paints. Very good hiding power as an organic pigment. As it has good rheological properties, it can be used even at high pigment concentrations (about 20 % relative to solid binder) without any effect on gloss. Eminently suitable for the production of intense opaque yellow shades for lead-free or low-lead paints. Not suitable for stoving enamels because of the high risk of blooming

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Suitable for the production of intense opaque yellow shades for lead-free or low-lead paints.