CC.Fast Yellow 5GP07

- PRODUCT:

Name			:  CC.Fast Yellow 5GP07

Chemical Class		:  Mono Azo

Colour Index Name	:  Pigment Yellow 74

Colour Index No.		:  11741

CAS No.		:  6358-31-2

EINECS No.		: 228-768-4

Substance Name		: 2-[(2-methoxy-4-nitrophenyl)azo]-N-(2-methoxyphenyl)-3-oxobutyramide

Molecular Formula	: C18H18N4O6

- PHYSICAL PROPERTIES:

Density		:   1,4 - 1,5 gr / cm³		Specific Surface		: 18 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  50 - 55 ml / 100 g

pH 		:  6 to 8

Heat stability       :  140 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 140 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 5

- WEATHER FASTNESS  :

6 Months	:  5 - 4				12 Months		   : 4

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 3 - 4 		Butyl Acetate	: 3		DOP	: 4

Toluene		: 4 		White Spirit 	: 5		DBP	: 4 - 5

Paraffin Wax	: 4 - 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 5		Cellosolve:

- TECHNICAL COMMENTS:

CC.Fast Yellow 5GP07 is a very strong, highly opaque, green shade monoazo yellow. The shade is similar to Pigment Yellow 1, but with higher colour strength, transparency and gloss. Yellow pigment with good fastness to light and weathering for air-drying paints. Very good hiding power as an organic pigment. As it has good rheological properties, it can be used even at high pigment concentrations (about 20 % relative to solid binder) without any effect on gloss. Eminently suitable for the production of intense opaque yellow shades for lead-free or low-lead paints. Not suitable for stoving enamels because of the high risk of blooming

- APPLICATIONS:

Recommended for paste inks as well as for solvent- and water based packaging gravure and flexographic printing inks.

Suitable for the production of intense opaque yellow shades for lead-free or low-lead paints. Not suitable for stoving enamels because of the high risk of blooming.