CC.Fast Yellow H10G

- PRODUCT:

Name			:  CC.Fast Yellow H10G

Chemical Class		:  Disazo Pigment

Colour Index Name	:  Pigment Yellow 81

Colour Index No.		:  21127

CAS No.		:  22094-93-5

EINECS No.		: 244-776-0

Substance Name		: 2,2'-[(2,2',5,5'-tetrachloro[1,1'-biphenyl]-4,4'-diyl)bis(azo)]bis[N-(2,4-dimethylphenyl)-3-oxobutyramide]

Molecular Formula	: C36H32Cl4N6O4

- PHYSICAL PROPERTIES:

Density		:   1,4 - 1,45 gr / cm³		Specific Surface		: 18 m² / gr

Moisture Content  : Max. 1%			Water Soluble Content	: Max. 1%

Oil Absorption     :  60 - 65 ml / 100 g

pH 		:  6 to 8

Heat stability       :  180 C° / 5 min. (Full Tone)             Tint Tone (1:10)		: 150 C° / 5 min.

Acid Resistance	: 5				Alkali Resistance		: 5

- LIGHT FASTNESS  :

Full Tone (1:1)	:  7 - 6				Tint Tone (1:10)		   : 6

- WEATHER FASTNESS  :

6 Months	:  3 - 4				12 Months		   : 3

- FASTNESS PROPERTIES:

Migration             : 4 - 5 (p-PVC)

Ethanol		: 5		Ethyl Acetate	: 4		MEK	: 4

Butanol		: 4 - 5		Butyl Acetate	: 4		DOP	: 4

Toluene		: 4 		White Spirit 	: 4 - 5		DBP	: 4

Paraffin Wax	: 5		Butter		: 5		Soap	:5

Water		: 5		Linseed Oil	: 4		Cellosolve:

- TECHNICAL COMMENTS:

Very greenish yellow pigment with substantially higher tinctorial strength than Pigment Yellow 3 which is similar in shade. It does not equal this pigment in its fastness to light and weathering but, because of its otherwise good properties, particularly its fastness to solvents and overpainting, it is suitable for all paint systems.

- APPLICATIONS:

Recommended for paints when stoving temperature does not exceed 200° C.